Table S8. Physicochemical properties of PEG-PBAE particles.

| NP | Hydrodynamic diametera SD(nm) | PDIaSD | -potentiallbSD(mv) |
| --- | --- | --- | --- |
| PEG-PBABE/miR-control | 70.24.7 | 0.160.03 | 2.80.8 |
| PEG-PBABE/miR-382 | 71.71.2 | 0.140.02 | 2.30.6 |
| PEG-PBABE/miR-340 | 70.71.0 | 0.120.02 | 1.80.7 |

aHydrodynamic diameter (number mean) and polydispersity index (PDI) were measured by dynamic light scattering (DLS) in 10 mM NaCl at pH 7.4. Mean SD(n=4). b-potential was measured by laser doppler anemometry in 10 mM NaCl at pH 7.4. Mean SD(n=4)